## Slide 1
Company & Product
Introduction
Intellect Pioneering Battery Tech Co., Ltd.

## Slide 2: Agenda
I、Company Introduction
II、Lithium-ion polymer cell Character & Performance
III、IP Product Introduction
1）RC Li-ion polymer Battery
2）LiFePO4 Power battery
3）Li-NMC Power battery
4）High Capacity Digital Li-ion polymer Cell
IV、Safety Performance

## Slide 3: I、Company Introduction

## Slide 4: Company Introduction
Established in 2007,Intellect Pioneering Battery Technology Co.,Ltd (IP) is having our headquarters in Hongkong ,and our production plant is located in Shunde District,FoShan ,GuangDong province, PRC, by which we enjoy the geographic convenience and fast transportation infrastructure.The company is having production space of 20,000 square meters and with daily production volume over 100,000Ah.
IP is an innovative Hi-Tech corporation with independent intellectual-property and core technologies, which is specialized in high power, high energy and environmental-friendly Lithium-ion polymer battery’s R&D ,Production and management. And our batteries are sold across Europe, America, Asia, and so on . Our product range includes high-rate RC battery series, high-power battery series ,high capacity digital products series. Our batteries are widely used in the remote-control electric airplane and cars,electric model-gun, power motorcycle starter battery, UPS power facilities devices,electric bicycle,electric motorcycle, and mobile phone,MP3/MP4,bluetooth,PDA,GPS,notebook PC, military products,and so on .
Since foundation , IP was growing with an annual turnover of 30-50% ,and has passed the ISO9001: 2008 system certification. And our products had passed the UN, UL, CE, ROHS certifications.

## Slide 5
It is our mission to offer high quality batteries, to strive as a leading brand in the same trade, creating real and long-lasting value for our customers, prompting career growth for our staff, and supplying clear and safe energy for society. Our vision is to turn ourselves as a prestige and worldwide leading battery export.
IP will be an international, high-tech and service-oriented enterprise in future.
Your Energy Partner!
Mission and Vision

## Slide 6
Certification

## Slide 7
Production Process
Materials Mixing and coating
Electrode-making
Winding & Stacking
Injection
And Sealing
Formation
And Grading
Storage
Final inspection
Packing

## Slide 8: Quality Control
Co-R&D with suppliers for main raw-materials
CE、UL、UN Certification
ISO9001:2008 Quality-Control System
QC Improvement System
Product Quality-control
Quality plan
Procedure Quality-control
Raw-materials Quality-control
Supplier’s Quality-control
ISO9001: 2008
CE
UN
UL
RoHS
Notes: 8

## Slide 9
Quality Control
Co-R&D with suppliers for main raw-materials
CE、UL、UN Certification
ISO9001:2008 Quality-Control System
QC Improvement System
Product Quality-control
Quality plan
Procedure Quality-control
Raw-materials Quality-control
Supplier’s Quality-control
ISO9001: 2008
CE
UN
UL
RoHS

## Slide 10: II、Lithium-ion polymer cell Character & Performance

## Slide 11
Comparison of different types battery

## Slide 12
Performance Comparison different Positive electrode
Item | LiFePO4 | Li(NiaMnbCoc)O2 | LiMn2O4 | LiCoO2
Theoretical specific energy (mAh/g) | 170 | >190 | 148 | 274
Actual specific energy (mAh/g) | 130 | 150 | 90 | 145
Discharge platform (V) | 3.2-3.3 | 3.6-3.7 | 3.7-3.8 | 3.6-3.7
Cycle life (times) | >2000 | >1000 | >300 | >500
High temperature performance(℃) | >75℃ | >65℃ | ~45℃ | ~80℃
High rates performance | better | good | bad | better

## Slide 13: III、IP Product Introduction

## Slide 14: High Rate RC battery introduction

## Slide 15
Unique Technical Structure
----Winding & Stacking
Integrate and consolidate advantages of the winding structure and the stacking structure , avoid and reduce the negative factors of both

## Slide 16: Advantages of IP high rate battery
Unique Technical Structure：Winding & Stacking
Integrate and consolidate advantages of the winding structure and the stacking structure ,avoid and reduce the negative factors of both
Technical Structure | Advantages | Application | Disadvantages
Stacking | Low internal resistance（parallel connection structure） High energy density | Stable high voltage and high power Small volume ,light weight | High probability of internal short-circuit Bad consistency
Winding | Low probability of internal short-circuit Good consistency | High reliable quality ；high yield rate | High internal resistance（series connection structure） Energy density is lower than 5%

## Slide 17: Power character of High Rate battery
High Rate Range: 10C--50C
Typical 40C cell design
Continuous Discharge ：5000Wh/kg and 10000Wh/L
Pulse Discharge： 8000Wh/kg and 16000Wh/L

## Slide 18: IP high rate battery character

## Slide 19: IP high rate battery cycle life character

## Slide 20: IP LiFePO4 Power Battery Introduction

## Slide 21: Features of IP LiFePO4 Power Battery
Long Cycle Life
Outstanding rated discharge performance
Excellent low temperature performance

## Slide 22: Typical Charging Curve

## Slide 23: Typical Rated Discharging Curve

## Slide 24: Excellent low temperature performance

## Slide 25: Comparison under different Temperatures at different Rates
Even at low Temperature, IP battery is still strong powerful！

## Slide 26: Single cell charge-discharge at 1C Cycle Performance＞1500 times (room temperate )

## Slide 27: Single cell charge-discharge at 1C Cycle Performance＞500 times (55℃)

## Slide 28: 12S battery pack discharge at 1C Cycle Performance＞1500 times (room temperate )

## Slide 29: Li-NMC Power battery Introduction

## Slide 30
Cell Performance curve
Charge curve
Discharge curve
The capacity decrease at app. 0.15% per month
storage

## Slide 31
Cell Performance curve
1C Cycle Performance @55℃
1C Cycle Performance @5℃
3C Cycle Performance @25℃
1C Cycle Performance @25℃c

## Slide 32
Battery Pack Performance curve

## Slide 33: High capacity digital cell introduction

## Slide 34
Features：High、Hard、Smooth
High-High Volumetric Energy Density、High Safety
1、High energy density, high gram capacity, high safety materials 2、Highly active substances content formula
3、High security structure design
Hard- The body of cell is so hard that it can be wrapped directly by sticker instead of the Plastic shell.
1、Special Ageing technology
2、Special Sealing technology
Smooth-The body of cell is smooth as mirror surface
1、Special winding structure 2、Special electrode design
Notes: 34

## Slide 35
Energy Density Road Map
Note: calculated by model of 454261
Notes: 35

## Slide 36
Typical charge-discharge Curve
At 0.5C , charged into 90% capacity already only after CC.
Notes: 36

## Slide 37
Typical Rate Discharging Curve
Notes: 37

## Slide 38
Low temperature Performance
Notes: 38

## Slide 39
Cycle life Performance
Notes: 39

## Slide 40: IV、Safety Performance

## Slide 41: Standard Safety Testing Demo（LiFePO4)
Nail Test
Short-Circuit
Overcharge

## Slide 42: Nail Test Demo of IP standard power battery
A. Before Testing
B.1minute later after Nail Test（punctured 3 nail rapidly）
C.5 minutes later after Nail Test
D.10 minutes later after Nail Test
E.30 minutes later after Nail Test
F.60 minutes later after Nail Test
G.120 minutes later after Nail Test
H.Finish Nail Test (242 minutes later)
Notes: 42

## Slide 43: Short-circuit Demo of IP standard power battery
A Before Test
B In Short-circuit
C After Test 1
D After Test 2
★★★ Note:
Directly short circuit，the highest temperature is 30.3℃，the temperature increased 4.7℃and the voltage decreased 0.146V。

## Slide 44: Overcharge Demo of IP standard power battery
Chart: 1C12V过充U-I-T曲线
电流 | 10 | 10.001 | 10 | 10 | 9.999 | 10.001 | 10 | 10 | 10 | 9.999 | 9.999 | 10.001 | 10.001 | 10.001 | 10.001 | 1.096 | 0.852 | 0.793 | 0.813 | 0.858 | 0.887 | 0.917 | 0.925 | 0.932 | 0.942 | 0.953 | 0.843 | 0.856 | 0.858

## Slide 45
IP will grow with you!